## Slide 1: Subsurface Geochemical Rock-Fluid Interactions in Caney Shale, South-Central Oklahoma Oil Province (SCOOP)
Gabriel Awejori1, Wenming Dong2, Christine Doughty2, Nicolas Spycher2 , Fengyang Xiong1 and Mileva Radonjic1,3
1Geomimicry and Barrier Materials Labs, School of Chemical Engineering, Oklahoma State University, Stillwater, OK 74078, USA
2Energy Geosciences Division, Lawrence Berkeley National Laboratory, 1 Cyclotron Road, Berkeley, CA 94720, USA
3Boone Pickens School of Geology, Oklahoma State University, Stillwater, OK 74078, USA
DOE Award DE-FE0031776 from the Office of Fossil Energy in Partnership with Industry Partner, OGS, OSU Geology, OSU Chem. Engineering, University of Pittsburgh, Lawrence Berkeley National Lab and DOE NETL.

## Slide 2: PRESENTATION OUTLINE
Introduction
Objectives
Materials
Methodology
Results and Discussions
Conclusions
Fig. 1: SEM micrograph of reacted powder sample showing rock grains and clay sized particles.
Clay
Quartz
Carbonate

## Slide 3: INTRODUCTION
The Caney Shale is located in the Ardmore Basin of South-Central Oklahoma Oil Province (SCOOP)
It overlies the better-known Woodford Shale which has been the main target of drilling in the area over the years
The Caney Shale, though replete with hydrocarbons, is characterized by high clay content, complex mineralogy, and ultra-low permeability
This makes hydraulic fracturing the most viable option in producing from this shale
This study characterizes the long-term geochemical responses of the Caney Shale after hydraulic fracturing
Fig. 2: Geological map of Oklahoma, showing SCOOP area (red ellipsoid) and well locations (red star) (after Johnson, 2008)

## Slide 4: OBJECTIVES
This work is designed to investigate the impact of geochemical rock-fluid reactions on permeability of Caney Shale
The following sub-objectives culminate in achieving this objective:
Evaluate the mineralogy of the Caney Shale
Observe and assess mineralogical changes in the Caney Shale due to rock-fluid reaction, post-hydraulic fracturing
To investigate mechanisms driving mineralogical transformations post-hydraulic fracturing
Fig. 3: Fracture and near-fracture Rock-Fluid Interaction following hydraulic fracturing of reservoir formation

## Slide 5: MATERIALS
Rock samples used for this experiment are recovered from two different wells as follows:
Well 1:
  Vertical well across entire Caney Shale
  Samples are recovered as cored-rock
Well 2:
  Horizontal well drilled within Reservoir 3
  Samples are recovered as rock-cuttings at 1000ft intervals
Rock samples are prepared and ground into powders with average particle size of 30µm
Produced fluid recovered from Caney Shale was the main reacting fluid. Deionized water was used as a standard for comparison
Fig. 4: Relative positions of two wells and sample locations: Samples W11 to W15 are cored-rocks from five (5) zones of the formation. W21 to W23 are rock cuttings spaced 1000ft horizontally at approximately the same vertical depth (Schematic not drawn to scale)
W11
W12
W13
W14
W15
W21
W22
W23
Well 1
Well 2
Reservoir 1
Ductile 1
Reservoir 2
Reservoir 3
Ductile 2

## Slide 6
METHODOLOGY
Rock Powder
Fluids
Oven
X-ray Diffraction (XRD)
Scanning Electron Microscopy/ Energy Dispersive Spectroscopy (SEM/EDS)
Before
After
Mineralogical Compositions
Chemical Compositions
Microstructure
Characterization of Alterations caused by Geochemical Reaction
SAMPLE PREPARATION AND STATIC BATCH REACTOR EXPERIMENT
LABORATORY TECHNIQUES AND DATA ACQUISITION
DATA ANALYSES, INTEGRATION AND INTERPRETATION
Vertical Well (Cored-Rock)
Horizontal Well (Rock-Cuttings)
Main Fluid: Field Produced Fluid
Standard: Deionized Water
Conditions: 95oC (203oF), 14.7psi
Liquid to powder ratio (150mL:1g) Average Particle Size =30µm
Sampling Days: 0, 7 and 30 days
Flow chart of materials and methodology adopted for experiment, data acquisition and interpretation
Inductively Coupled Plasma Mass Spectroscopy (ICPMS)

## Slide 7
RESULTS - Mineralogical Alterations in Well 1 Samples
Pyrite dissolution occurs within the first 7 days of reaction
Quartz reduces in the first 7 days but increases between 7 to 30 days whilst carbonate is relatively stable
Feldspar composition reduces and completely breakdown after 30 days
Illite composition shows an increasing trend over 7 days but remains relatively the same between 7 days and 30 days
W1 – Vertical Well
W2 – Horizontal Well
(7) – 7 days reaction
(30) – 30 days reaction

## Slide 8
RESULTS - Mineralogical Alterations in Well 2 Samples
Pyrite breakdown occurs within the first 7 days of reaction
Composition of quartz drops after 7 days but increases between 7 to 30 days
Feldspar reduces continuously and mostly dissolve or transform by 30 days
Illite composition shows an increasing trend after 7 days reaction and decreases between 7 and 30 days
W1 – Vertical Well
W2 – Horizontal Well
(7) – 7 days reaction
(30) – 30 days reaction

## Slide 9
RESULTS – Ternary Diagram
Comparison of unreacted samples to 7 days and 30 days reacted samples – Produced Fluids
The ternary diagram gives a big picture of impacts of mineralogical changes on rock properties
Mineralogy of rocks are originally closer to quartz and pyrite, indicating brittleness
Rock-fluid reaction shifts the samples to phyllosilicate zone, indicating ductility
Ductility promotes fracture healing thus loss of permeability
Main reactions that promote shift include:
  Breakdown of pyrite and microcrystalline quartz
  Breakdown of feldspar and carbonates
  Formation of illite

## Slide 10: RESULTS – Comparison of XRD Diffractograms
Amorphous content generated after reaction is observed in the clay portions of the diffractogram
Large increase in amorphous content occurs in first 7 days of reaction
High amorphous compositions in the clay section possibly due to deflocculation and dispersal of illite
Graph shows XRD diffractograms (right: zoomed-in) of unreacted and reacted samples from W2
Peak intensities of quartz and carbonates show significant reductions after 7 days reaction
Reduction mainly due to breakdown of the minerals
i/s
i
q
q
h/ps
d
c
q
q
h/ps
i/s
i
a
q
ii
q
q
c

## Slide 11: RESULTS – SEM micrographs and EDS Plots
Following slide compares elemental concentrations of spots selected on unreacted and reacted samples
Microanalysis of all the samples are carried out under the same set of conditions
Spectrum 6 in all samples is selected to record data for substrate used to hold samples – mainly carbon
Left: Unreacted sample have highest concentrations (highest peaks) of elements forming the major minerals in samples- oxygen, silicon, aluminum and calcium
Middle: Samples reacted for 7 days show moderate concentrations for major elements in samples. This indicates mineral breakdown or transformation
Right: Samples reacted for 30 days show similar concentrations of major elements as 7 days reacted samples. This is because the reactions and transformation of minerals within these periods are relatively less
Note:
The shortfall of these measurements is inability to repeat spot analyses on the exact particles for both pre-reaction samples and post-reaction samples
However, since particles in powders have comparable mineralogy, multiple spots helps to minimize errors from heterogeneity

## Slide 12: RESULTS – SEM micrographs and EDS Plots
W22_Unreacted_Spot
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
W22_7days_Spot
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
W22_30days_Spot
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si

## Slide 13
RESULTS - Chemical Composition of Caney-Produced Fluids Effluent (ICPMS)
Due to approximate neutral pH, Ca concentrations relatively stable
Dissolution of carbonates occur due to transient acidity caused by dissolution of pyrite
Precipitation or cation exchange in clay sites may lead to Ca uptake from effluent causing decreased Ca concentrations
The high Si concentrations cannot be explained only by the dissolution of quartz at the experiment conditions
Dissolved biogenic (microcrystalline quartz) or amorphous silica could explain high silica concentrations
Dissolution of feldspar contributes to Si concentration in effluent
Al is mainly from the dissolution of feldspars
Al concentrations are very low due to uptake from fluid – illite and other Al-based mineral precipitation
Similar trends observed for Magnesium (Mg) and Iron (Fe)
Chart: Ca Concentration
| W11 | W12 | W13 | W14 | W15 | W21 | W22 | W23
0 days | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577
7 days | 406614.8321 | 441292.5619 | 403210.5147 | 466723.9245 | 394016.0823 | 421729.7828 | 428776.6468 | 463751.3979
30 days | 431069.7043 | 412014.7063 | 410863.8242 | 439798.5718 | 474640.5789 | 438092.808 | 456574.8855 | 469422.0262
Chart: Si Concentration
| W11 | W12 | W13 | W14 | W15 | W21 | W22 | W23
0 days | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354
7 days | 26156.7483 | 39861.674 | 34208.9818 | 26551.1619 | 22421.1461 | 26178.5648 | 40650.5829 | 24740.6883
30 days | 55978.7873 | 56257.7372 | 61934.8532 | 49012.8589 | 42277.2656 | 49179.5693 | 49306.7985 | 51828.4391
Chart: Al Concentration
| W11 | W12 | W13 | W14 | W15 | W21 | W22 | W23
0 days | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826
7 days | 170.4136 | 343.7413 | 171.2924 | 162.8403 | 103.8948 | 159.9444 | 156.1593 | 146.5187
30 days | 118.6244 | 102.6724 | 101.3618 | 90.4312 | 91.8806 | 99.3314 | 87.3453 | 84.6583

## Slide 14: RESULTS – Model of Experiment
Modeling of experiment shows most elemental concentrations in effluent matching with ICP-MS results
Due to limitations in complete characterization of rock and fluids, some assumptions were made in the model
These assumptions and limitations of model are captured in the next slide

## Slide 15: RESULTS – Model of Experiment
The following uncertainties and limitations are worth noting about modeling of experiment:
Thermodynamic data/models
  Modeled minerals of mixed composition (e.g. clays) may not have the same composition as in the rock formation
  Fluid salinity may exceed the validity range of the implemented ion activity model (extended Debye-Hückel)
Reconstruction of the Produced Fluid compositions
  Anion concentrations computed from assumptions Organic compounds besides acetate were neglected (unknown potential effects on experimental results)
Rock formation mineralogy
  Trace or amorphous minerals (undetected by XRD) impact the system geochemistry – amounts and types were assumed
Sampling effects
  Interactions with atmosphere (O2, CO2 impact pH and redox) Mineral reaction rates (kinetic constants, surface area)

## Slide 16: DISCUSSION
Illitization – Increased illite composition due to breakdown of feldspars which provides the necessary elements for illitization. This phenomenon has been observed in earlier studies such as Guven et al., (1982), where they observed that illitization is favored by high Al concentrations at circum-neutral pH. This is similar to conditions of our experiment
Iron Oxides – The breakdown of pyrite and other iron-bearing minerals release mostly, Fe(II) into solution which is subsequently oxidized to Fe(III) oxyhydroxides that block pores within the formation and lead to permeability losses. The breakdown of pyrite in this study points to high probability of iron oxides formation
Fines Migration – Clay fines migration are occasioned by the deflocculation and dispersal of clay minerals. These subsequently aggregate within flow paths to cause significant permeability losses. High amorphous compositions after reaction observed in this study points to possible clay deflocculation
The cumulative impact of reactions described above is the loss of permeability of formation during long-term post-hydraulic fracturing rock-fluid interactions.

## Slide 17: CONCLUSIONS
The following conclusions are drawn from the integration of results and discussions above:
Breakdown of pyrite and other sulfides after exposure to produced fluid led to generation of acids which temporarily reduce the pH of fluids, thus catalyzing breakdown of other minerals
Oxidation is a major mechanism driving precipitation of Fe(III) oxyhydroxides in post-hydraulic fracturing
Clay minerals deflocculation, dispersal and fines migration likely in Caney Shale during hydraulic fracturing. This can cause the blocking of flow paths, thus reducing fracture permeability
Increased illite composition induces ductility into an originally brittle rock which can lead to healing of fractures and thus loss of permeability. This is believed to be the cause of rapid permeability decline in most hydraulically fractured shale reservoirs.

## Slide 18: ACKNOWLEDGEMENTS
The authors acknowledge:
DOE Award DE-FE0031776 from the Office of Fossil Energy’s, Oil and Natural Gas Program, U.S. Department of Energy
Lisa Whitworth and Brent Johnson of Oklahoma State University Microscopy Laboratory for the support during data acquisition
Our industry partners for providing materials and Caney well production histories.

## Slide 19: REFERENCES
Awejori, G. A., Doughty, C., Xiong, F., Paronish, T., Spycher, N., Radonjic, M. (2022). Integrated Experimental and Modeling Study of Geochemical Reactions of Simple Fracturing Fluids with Caney Shale. Energy & Fuels, 36(17), 10064–10081.
Bratcher, J. C., Kaszuba, J. P., Herz-Thyhsen, R. J., Dewey, J. C. (2021). Ionic Strength and PH Effects on Water–Rock Interaction in an Unconventional Siliceous Reservoir: On the Use of Formation Water in Hydraulic Fracturing. Energy & Fuels, 35(22), 18414–18429.
Chakraborty, N., Karpyn, Z. T., Liu, S., Yoon, H. (2017). Permeability evolution of shale during spontaneous imbibition. Journal of Natural Gas Science and Engineering, 38, 590–596.
Farrokhrouz, M., Taheri, A., Iglauer, S., & Keshavarz, A. (2022). The influence of acidizing on propped fractures for productivity enhancement: Eagle Ford laboratory study. Fuel, 329. https://doi.org/10.1016/j.fuel.2022.125363
Jew, A. D., Druhan, J. L., Ihme, M., Kovscek, A. R., Battiato, I., Kaszuba, J. P., Bargar, J. R., Brown Jr, G. E. (2022). Chemical and Reactive Transport Processes Associated with Hydraulic Fracturing of Unconventional Oil/Gas Shales. Chemical Reviews, 122(9), 9198–9263.
Li, Q., Jew, A. D., Kohli, A., Maher, K., Brown Jr, G. E., Bargar, J. R. (2019). Thicknesses of chemically altered zones in shale matrices resulting from interactions with hydraulic fracturing fluid. Energy & Fuels, 33(8), 6878–6889.
Mukhina, E., Cheremisin, A., Khakimova, L., Garipova, A., Dvoretskaya, E., Zvada, M., Kalacheva, D., Prochukhan, K., Kasyanenko, A., Cheremisin, A. (2021). Enhanced oil recovery method selection for shale oil based on numerical simulations. ACS Omega, 6(37), 23731–23741.
Swami, V., Clarkson, C. R., Settari, A. T. (2012). Non-Darcy flow in shale nanopores: do we have a final answer? SPE Canadian Unconventional Resources Conference.

## Slide 20: THANK YOU
For further enquiries, suggestions and questions, please reach out to us on:
gabriel.awejori@okstate.edu
mileva.radonjic@okstate.edu