## Slide 1: CHEMICAL REACTIVITY OF CANEY SHALE TO KCL-BRINES AT ELEVATED TEMPERATURE AND PRESSURE
Presenter: Gabriel Adua Awejori
Awejori, G.A., Fengyang, X., Luo, G., Grider, C., Katende, A., Radonjic, M.
Oklahoma State University, Stillwater, Oklahoma, USA
Doughty, C., Spycher, N.
Energy Geosciences Division, Lawrence Berkeley National Laboratory, Berkeley, California, USA
Paronish, T.
Leidos Research Support Team, National Energy Technology Laboratory, Morgantown, West Virginia, USA
O’Connell, L.
Stim-Lab Inc., Duncan, Oklahoma, USA
Rihn, A.
Continental Resources, Oklahoma City, Oklahoma, USA
DOE Award DE-FE0031776 from the Office of Fossil Energy in Partnership with Continental Resources, OGS, OSU Geology, OSU Chem. Engineering, University of Pittsburgh, Lawrence Berkeley National Lab and DOE NETL.
AIChE Annual Meeting 2021, BOSTON, MASSACHUSSETS

## Slide 2: PRESENTATION OUTLINE
Introduction
Objectives
Materials and Methodology
Results
Conclusions and Recommendations
Retrieved Core from Caney Shale on Display

## Slide 3: SUMMARY
Geochemical reactions between rocks and engineered fluids impact petrophysical properties of a formation
The impacts of these reactions are particularly prominent in micro-fractures and nano-fractures (scale) as opposed to geomechanical forces which act more on macro-fractures more
Micro-fractures and nano-fractures form extensive networks that reach deep into the reservoir thus very important
They serve as conduits for hydrocarbon transport to the main fractures and then to the well
Therefore, any adverse rock-fluid interactions in these zones can greatly reduce permeability thus, productivity from a reservoir
This research focuses on rock-fluid interactions and their adverse outcomes as well as geomechanical stress impacts on fracture face
Our work focuses on Caney Shale play South Central Oklahoma Oil Province

## Slide 4: INTRODUCTION
The Caney shale is a newly discovered unconventional reservoir in South Central Oklahoma
Though known to contain substantial amounts of hydrocarbon, it was designated a seal and/or source rock due to its high clay content
Advancements in hydraulic fracturing technologies has however unveiled the potential of the Caney Shale
Recent drilling and exploitation has revealed adverse rock-fluid interactions in the formation
Geochemical characterization is essential to understanding these interactions and to improving recovery efficiency

## Slide 5: OBJECTIVES
Investigate rock responses to HFFs. Key concerns are:
Migration of fines (Caney shale has high illite composition)
Swelling clays and detachment of clay layers
Dissolution and precipitation of minerals
Impact of these in occluding fractures and cutting of the connection between well and reservoir

## Slide 6
Characterization of Rock-Fluid Interactions
Modelling (TOUGHREACT)
Batch Experiment and Conductivity Test
CT Scan and X-Ray Fluorescence
Enable Long-Prediction
From Pore to Core
Three-Pronged Approach: Experiment, Simulation and Logging
MATERIALS AND METHODLOGY
X-Ray Diffraction- Mineralogical Composition
Inductively Coupled Plasma-Mass Spectrometry – Effluent Analysis
Scanning Electron Microscopy - Dissolution and Precipitation Patterns

## Slide 7
Materials Used:
Three fluid samples of varying compositions:
2% Potassium Chloride Solution (pH~4)
0.5% Choline Chloride Solution (pH~4)
Deionized Water (Base, pH~7)
Three rock samples selected at different depths:
High Quartz (HQ)
    [74.4% Quartz, 9.6% Carbonate and 16% Clay]
Moderate Quartz, Carbonate and Clay (MQ)
    [63.1% Quartz, 17.1% Carbonate and 19.8% Clay]
High Clay (HC)
    [41.5% Quartz, 14.1% Carbonate and 44.4% Clay]
MATERIALS AND METHODLOGY
Batch Experiment
Designed to mimic shut-in period
Undertaken at Temperature of 90oC and atmospheric pressure
Initial Liquid to powdered sample ratio of 20:1 (140mL:0.7g)
Sampling done on days: 1, 4, 7, 14, 21 and 28 (10mL sample)
Conductivity Test
Proppant (40/70) sandwiched between half piece of core sample
Changing Stresses applied, 4000-12000 and back to 4000
Width, Permeability and Conductivity measured

## Slide 8
Identifying the key driving force that can cause varying outcomes for rock-fluid interactions
Question: Is it the fluid or it is the rock?
Answer: Obviously the fluid
RESULTS
Impact of Fluid Composition on elemental concentration in effluent
Impact of Rock Composition on Elemental Concentration in effluent

## Slide 9
Calcium ion:
Ca ion concentration distinguishable for each fluid type
Ca ions in solution believed to be from Calcite and Dolomite Dissolution
Potassium Chloride>Choline Chloride>Deionized water (In terms of ion concentration in solution)
HQ and MQ samples have higher concentrations than HC sample
RESULTS

## Slide 10
RESULTS
Sulphate ion:
SO4 ion concentration distinguishable for each fluid type
SO4 ions in solution believed to be mainly contributed from the Dissolution of Pyrite
Potassium Chloride>Choline Chloride>Deionized water (In terms of ion concentration in solution)
HQ and MQ samples have higher concentrations than HC sample
Chart: HQ
| 1 | 3 | 7 | 14 | 21 | 28
HQDI | 10.649 | 15.642 | 21.623 | 29.333 | 31.7 | 36.045
HQKCl | 23.188 | 30.817 | 35.835 | 40.306 | 39.8 | 43.905
HQCCl | 11.902 | 16.732 | 23.548 | 31.077 | 32.5 | 33.368
Chart: MQ
| 1 | 3 | 7 | 14 | 21 | 28
MQDI | 8.989 | 14.198 | 22.363 | 29.5 | 30.1 | 33.013
MQKCl | 18.173 | 25.431 | 32.078 | 36.243 | 34.7 | 40.563
MQCCl | 12.624 | 17.811 | 26.535 | 33.605 | 33.6 | 35.278
Chart: HC
| 1 | 3 | 7 | 14 | 21 | 28
HCDI | 10.079 | 14.307 | 17.89 | 20.312 | 20.5 | 22.451
HCKCl | 11.511 | 15.372 | 18.007 | 19.557 | 19.2 | 20.711
HCCCl | 9.328 | 13.32 | 17.947 | 21.795 | 21.7 | 22.251

## Slide 11
Silicon ion:
Si ion concentration for various fluids clearly distinguishable
Si ions in solution believed to be from quartz and clay minerals
Potassium Chloride>Choline Chloride>Deionized Water (In terms of ion concentration in solution)
Si ions most likely from the clay and feldspathic component of the rock
RESULTS

## Slide 12
Al and Mg ions show sharp decline in concentrations: Two theories exists:
  Precipitation
  Substitution or Adsorption
Aluminum elements in solution are from dissolution and cation exchange in clay minerals
Magnesium elemental concentration is mainly from dissolution of dolomite, but clay dissolution and cation exchange in clays may also contribute
RESULTS

## Slide 13: RESULTS
Stress Impact on Width, Permeability and Conductivity
Chart: Confining Stress
| 2000 | 4000 | 6000 | 8000 | 10000 | 12000 | 6000 | 4000
D22 | 4000 | 2769.2308 | 2583.3333 | 2054.0541 | 1800 | 1596.1538 | 1729.1667 | 1729.1667
R31 | 2875 | 1818.1818 | 2103.4483 | 1853.6585 | 1627.451 | 1535.7143 | 1666.6667 | 1603.7736
R32 | 1666.6667 | 1650 | 2142.8571 | 1804.878 | 1600 | 1438.5965 | 1607.8431 | 1547.1698
D21 | 2333.3333 | 2473.6842 | 2300 | 1975 | 1596.1538 | 1416.6667 | 1545.4545 | 1574.0741

## Slide 14: RESULTS
40/70 + Ductile 2-2, 3B & 6A |  |  |  |  |  |  |  | 
Stress (psi) | 2000 | 4000 | 6000 | 8000 | 10000 | 12000 | 6000 | 4000
Conductivity (md-ft) | 1376 | 952 | 428 | 150 | 62 | 25 | 31 | 32
40/70 + Reservoir 3-1, 2B & 7A |  |  |  |  |  |  |  | 
Stress (psi) | 2000 | 4000 | 6000 | 8000 | 10000 | 12000 | 6000 | 4000
Conductivity (md-ft) | 1263 | 878 | 481 | 208 | 76 | 37 | 40 | 41
40/70 + Reservoir 3-2, 2B & 7A |  |  |  |  |  |  |  | 
Stress (psi) | 2000 | 4000 | 6000 | 8000 | 10000 | 12000 | 6000 | 4000
Conductivity (md-ft) | 1466 | 948 | 435 | 173 | 70 | 32 | 36 | 39
40/70 + Ductile 2-1, 2B & 7A |  |  |  |  |  |  |  | 
Stress (psi) | 2000 | 4000 | 6000 | 8000 | 10000 | 12000 | 6000 | 4000
Conductivity (md-ft) | 1451 | 744 | 301 | 118 | 43 | 20 | 22 | 23
Stress Effect on Conductivity

## Slide 15
Chart: High Clay_DI
pH (25C) | 7 | 8 | 8 | 7.75 | 7.9 | 8.8 | 9.1
Chart: High Clay_KCl
pH meas (25C) | 4 | 7.9 | 8 | 8.1 | 8.6 | 8.9 | 9
Cooled atm CO2 | 4 | 8.054 | 8.071 | 8.097 | 8.122 | 8.138 | 8.088
Except pH values, modelled values and experimental values showed significant disparities
RESULTS
Chart: High Clay _KCl
Al | 0 | 3.6694e-06 | 0 | 0 | 0 | 0 | 0
Chart: High Clay _ KCl
Si | 0 | 0.00033138 | 0.0014883 | 0.0029741 | 0.0033585 | 0.0037422 | 0.0036852

## Slide 16
Three informal Divisions based on XRF results:
Upper Caney shows decreased Si concentration through heavily bioturbated intervals and Al and Fe rich intervals (Clay and Carbonate Rich Zone)
For the middle Caney, Al and Si concentrations remain consistent whilst Ca is low (Quartz-rich shale zone)
In the lower Caney, sharp increase in Ca is observed whilst Al and Si constant (Carbonate zone followed by High Quartz Shale)
RESULTS

## Slide 17: CONCLUSIONS AND RECOMMENDATIONS
Conclusions:
Rock-fluid interaction during hydraulic fracturing is largely the function of fluid composition
Carbonates and Clays are more susceptible to geochemical interactions whilst Quartz is relatively stable
Increasing clay composition in samples impact dissolution of quartz and carbonate minerals thus less fracture opening
Potassium Chloride and Choline Chloride stabilized clay minerals
Mechanism of stabilization is continuous exchange of ions between clays and fluid
This will help prevent swelling and disintegration of clays thus micro and nano-fractures remain open
Sustainability of stabilization looks unlikely??
Substitution of ions may be responsible for low Al and Mg ion concentration since these ions are both exchangeable cations
Stress has an impact on permeability and conductivity, though limited
Conductivity of ductile samples is higher per unit change in fracture width
Recommendations:
Working on improving geochemical and physical characterization for modelling in our next work
Further work to be done to clearly understand Al and Mg ion concentration trends
Longer experiments to determine the limits of effectiveness of temporary clay stabilizers considering pH values continued increasing for entire batch experiment

## Slide 18: ACKNOWLEDGEMENTS
The authors acknowledge:
DOE Award DE-FE0031776 from the Office of Fossil Energy’s, Oil and Natural Gas Program, U.S. Department of Energy
Joseph Renk, Technical Project Officer, National Energy Technology Laboratory
Lisa Whitworth and Brent Johnson of Oklahoma State University Microscopy Laboratory
Adam Haecker and Barry Dean of Continental Resources for providing Caney well production histories.
The authors would also like to thank George King for guidance
Vissa Vamsikrishna and Cody Massion of Oklahoma State University

## Slide 19: REFERENCES
Dove, P.M. 1995. Kinetic and thermodynamic controls on silica reactivity in weathering environments, in: White, A.F. and Brantley, S.L. (eds). Chemical Weathering Rates of Silicate Minerals. pp. 235–290.
Knauss, K.G., and T.J. Wolery. 1988. The dissolution kinetics of quartz as a function of pH and time at 70 C. Geochim. Cosmochim. Acta 52, 43–53.
Olabode, A.O. 2017. Diagenesis and Formation Stress in Fracture Conductivity of Shaly Rocks; Experimental-Modelling Approach in CO2-Rock Interactions.
Tester, J.W., W.G. Worley, B.A. Robinson, C.O. Grigsby, and J.L. Feerer. 1994. Correlating quartz dissolution kinetics in pure water from 25 to 625C. Geochim. Cosmochim. Acta 58, 2407–2420.