## Slide 1
Introduction
Purpose
To achieve a close to perfect isolation with wellbore cement between casing and rock formation, and later for plugging and abandonment after production for completed, halted and discarded wells.
To have a stable structure that withstands subsurface temperatures, pressures and loads (forces) while maintaining the reduced porosity and permeability. Sustaining wellbore cementing integrity for CO2 and H2 storage applications, possible prevention of methane leakage.
Research Problem
Wellbore cementing could possibly encounter formation and drilling fluids that contaminate and effect the stability of the structure, penetration and reaction of cement phases by exposure of sulphate or chlorine ions from the fluids thereby forming microcracks or scales.
The potential problem with graphene nanoplatelets GNPs application is their hydrophobic nature, leading to dispersion issues in cement slurries.
Objectives
To investigate how well dispersed liquid GNPs might contribute to cement hydration vs dry powdered GNPs that are not perfectly dispersed undergoing hydration for 7 and 28 days at simulated reservoir conditions.
To analyze the hydration of Portland cement-based slurry prepared with 15-30% of mixing water replaced by formation brines, in conjunction to exposure of fracturing fluids during hydration.
Jupudi, H., Massion, C., Johnson, B., and Radonjic, M.. (2022). Microstructural and Petrophysical Evaluation of Graphene Modified Portland Wellbore Cement Undergone Cyclic Temperature Loading. Geothermal Resources Council Transactions, Vol 46, paper ID#245.
Awejori, G., Barnett, L., Massion, C., Aldushaishi, M., and Radonjic, M. (2022). Chemical and Mechanical Stability of Cement during Fluid Invasion in Hydraulic Fractured Geothermal Wells. Geothermal Resources Council Transactions, Vol 46, paper ID#260.
Refining Wellbore Cement Stability during Development, Production and Abandonment of Unconventional Wells
Havila Jupudi1, Gabriel Awejori1, Cody Massion1, Mileva Radonjic1,2
1Petroleum Program, School of Chemical Engineering, College of Engineering Architecture and Technology, Oklahoma State University, Stillwater, OK, 74078
2Boone Pickens School of Geology, Oklahoma State University, Stillwater, OK, 74078
Results
Discussion
Key Findings and Future Work
Bibliography
Materials and Methodology
Materials
Graphene nanoplatelets (GNPs) prepared from environmental waste (PG) was provided by NovaGraphene. Graphene dispersed in 6wt% in water (LG) having an average of 4-6 layers, 99.5% pure is from US Research Nanomaterials.
Produced fluids, composition unknown were provided from an unconventional shale in Oklahoma.
Cement Samples Mix Designs
Water, bentonite, cement friction reducer and defoamer were added mixed by weight of cement (bwoc) to Class H cement powder to make the 0% GNPs control slurry. These were mixed following API Standard 10B to achieve a w/c ratio of 0.384 and 1965.15 kg/m3 (16.4 ppg) slurry.
Various mix designs were prepared by incorporating additives to control cement composition.
0.008% and 0.1% bwoc of powdered and liquid graphene
15% and 30% of produced water with hydration in calcium hydroxide solution (C) and fracturing fluid (F)
Molding and Thermal Cyclic Curing
The neat and mix design slurries were poured into 1×2.5 in molds and covered with a cling wrap to contain the moisture. These samples were left to hydrate for about 24 hours at room conditions .
The samples are instantly put into ̴pH13 Ca(OH)2 solution to prevent calcium leaching. The immersed cores sealed tight using aluminum foil and plastic wrap are then placed in an environmental chamber running between 20 oC and 110 oC at 95% relative humidity on an 8- hour cycle. The cement samples were cured for 21 and 84 cycles.
Sample preparation: cutting and polishing
A slab saw was used to cut the cores for desired size and to remove the uneven edges. A developed procedure was used for grinding and polishing the sample surfaces using water-free lubes. Later a bath sonicator was used for about a minute to remove any cement particles or polishing lubes. These samples are then dried at 50 oC for 2-3 hours.
Contact Information
Mileva Radonjic: mileva.radonjic@okstate.edu, Phone:(202)203-8973
GNPs Enhanced Cement
Based on previous studies GNPs were found to occupy the pore spaces and strengthen the weak points present in the core samples
GNPs are hydrophobic and inert thus inhibiting hydration of cement phases where it might have influenced CSH structure and chemical composition.
When harsher temperature change cyclic conditions were above 105 oC subjecting cement to retrogression, GNPs could have restricted the extension of microcracks.
Significant decrease in permeability and porosity were observed for all the samples hydrated at 28 days when compared to 7 days that could be explained due to the decrease in moisture content.
Hydraulic fracturing fluids Cement
Samples prepared in fracturing fluids showed lower permeability values when compared to those in Ca(OH)2 solution.
A low Ca/Si was observed that could have been due to the precipitation of the salt.
These trends change with dissolution of Friedel’s salt based on the fluid used for curing.
Cement durability in hot and cold cyclic conditions was tested with addition of graphene nanoplatelets and fracturing fluids.
Spot analysis using energy dispersive X-ray spectroscopy (EDS) line profiles showed trends of elements of phases on unhydrated grains and GNPs for micro reinforcement that could have resisted fracturing.
Back scattered electron micrographs showed more CSH gel like or hazy structures on 28 days hydrated cement samples.
Further evaluation of GNPs enhanced cement for X-Ray Diffraction (XRD), Focused ion-beam scanning electron microscopy (FIB-SEM), micro indentation, Raman spectroscopy and surface profilometry, and computed tomography (CT) will be done.
An initial low porosity and permeability was observed with fracturing fluids due to salt precipitation; subsequent dissolution gave higher values.
Increase in time for hydration increased the extent of hydration making it suitable for subsurface conditions.
Acknowledgements
The presenters wish to acknowledge:
DOE Award DE-FE0031776 from the Office of Fossil Energy and Continental Resources Inc.
Dr. Radonjic, PI, Hydraulic Barrier Materials Laboratory
Dr. Simon Iremonger, Sanjel Energy Services
Lisa Whitworth and Brent Johnson at Oklahoma State University Microscopy Laboratory.
Hydraulic Barrier Lab members for their support.
GNPs
Amorphous carbon
Figure 1: a) SEM images showing thin multiple platelets, rolled up and folded that of liquid graphene clustered together.
b) The irregular, sharp edges of platelets of powdered graphene about 200 µm in size with some amorphous rounded shaped structures that of carbon on them.
c) Energy dispersive x-ray spectroscopy (EDS) line profile on an unhydrated grain showing a decreasing trend of calcium, and silica. Carbon has a peak outside the grain confirming the presence of GNPs.
Figure 2: a) Porosity and permeability (µD) of neat and other mix designs after hydrated for 21 and 84 thermal cycles between 20 oC and 110 oC, 95% relative humidity. A significant decrease in the values were observed for 28 days in comparison to 7 days samples. b) GNPs are micro-reinforced within the pore spaces in the cement sample
Ca
Si
C
0.008%LG
Figure 3: a) 30% formation fluid contamination, cured in fracturing fluid for 7days b) Neat sample, cured in fracturing fluid for 7days.
Micro-pores in contaminated sample sealed by salts from highly saline formation fluid while neat sample is largely left porous.
Chart: 
28 days porosity | 24.1617 | 24.1679 | 27.9291 | 25.9286 | 21.6
28 days perm | 54.5431 | 43.1766 | 58.4665 | 72.1382 | 58.488
7 days porosity | 28.7556 | 29.7759 | 29.5515 | 29.6284 | 27.5
7 days perm | 91.5825 | 94.2823 | 89.097 | 87.1122 | 82.8726
Alite/Ferrite Composite
Pores
Outer CSH
Inner CSH
a
Alite/Ferrite Composite
Pores
Outer CSH
Inner CSH
b
Figure 4: a) Porosity of samples for 7days and 28days. b) Permeability (µD) of samples for 7days and 28days.
Hydration in neat cement samples follow the expected trend of decreasing porosity and permeability. However, competing effects of Friedel’s salts formation, dissolution and normal hydration effects control porosity and permeability in contaminated samples making their trends complex.
Chart: Porosity
| NC | NF | 15C | 15F | 30C | 30F
7days | 27.37 | 24.93 | 27.93 | 21.57 | 27.73 | 17.43
28days | 21.6 | 17 | 26.7 | 26.5 | 26.9 | 16.9
a
Chart: Permeability
| NC | NF | 15C | 15F | 30C | 30F
7days | 78.2099 | 68.8429 | 80.6102 | 32.956 | 75.8761 | 31.096
28days | 69.1198 | 81.9779 | 78.1673 | 82.6562 | 84.822 | 35.7651
b
b
a
c
a
GNPs embedded into the pore space
b