## Slide 1: Subsurface Geochemical Rock-Fluid Reaction in Caney Shale of Southern Oklahoma
Presenter: Gabriel Awejori
December 14, 2023

## Slide 2
Gabriel Awejori1
Wenming Dong2
Christine Doughty2
Nicolas Spycher2
Fengyang Xiong1
Mileva Radonjic1,3
1 Barrier Materials and Geomimicry Lab, School of Chemical Engineering, Oklahoma State University, Stillwater, OK 74978, USA
2Energy Geosciences Division, Lawrence Berkeley National Laboratory, 1 Cyclotron Road, Berkeley, CA 94720, USA
3Boone Pickens School of Geology, Oklahoma State University, Stillwater, OK 74078, USA

## Slide 3: PRESENTATION OUTLINE
Introduction
Objectives
Materials & Methodology
Results and Discussions
Conclusions
Fig. 1: SEM micrograph of rock-powder showing rock grains and minerals. (Ill-Illite, Qtz- Quartz, Cal – Calcite).
Qtz
Ill
Cal

## Slide 4: INTRODUCTION
The Caney Shale is an unconventional shale reservoir in the Ardmore Basin of southern Oklahoma
It overlies the Woodford Shale which is the more prominent producing shale in the area
Though Caney Shale host large reserves of petroleum, it is difficult to produce due to its ultra low permeability
Hydraulic fracturing is therefore employed to create sufficient permeability to enable production
This research is to gain insight on long-term geochemical responses of the Caney Shale after hydraulic fracturing
Location of Caney Well
Fig. 2: Geological map of Oklahoma, showing Ardmore Basin area and location of Caney Wells - Blue Star (Awejori et al., 2022)

## Slide 5: OBJECTIVES
This study investigates the geochemical rock-fluid reactions in subsurface Caney Shale and the impact of these on permeability in relation to production and carbon storage
To achieve this objective, crucial sub-objectives must be accomplished:
Evaluate and understand the mineralogical composition of the Caney Shale
Assess potential post-fracturing mineralogical transformations in the Caney Shale
Ascertain the mechanisms and factors controlling post-fracturing reactions and mineralogical transformations
Fig. 3: Fracture and near-fracture Rock-Fluid reactions following hydraulic fracturing of reservoir formation (Awejori et al., 2022)

## Slide 6
MATERIALS AND METHODLOGY
Rock Powder
Fluids
Oven
X-ray Diffraction (XRD)
Energy Dispersive Spectroscopy (EDS)
Inductively Coupled Plasma Mass Spectroscopy (ICP-MS)
Before
After
Mineralogical Compositions
Effluent Analyses
Chemical Compositions
Characterization of Alterations caused by Geochemical Reaction
SAMPLE PREPARATION AND STATIC BATCH REACTOR EXPERIMENT
LABORATORY TECHNIQUES AND DATA ACQUISITION
DATA ANALYSES, INTEGRATION AND INTERPRETATION
Vertical Well (Cored-Rock)
Horizontal Well (Rock-Cuttings)
Main Fluid: Field Fracturing
Fluid and Field Produced Fluid
Standard: Deionized Water
Conditions: 95oC (203oF), 14.7psi
Liquid to powder ratio (150mL:1g) Average Particle Size =30µm
Sampling Days: 0, 7 and 30 days
Flow chart of materials and methodology used in experiment, data acquisition and interpretation
Simulation
Modeling

## Slide 7
RESULTS – Mineralogical Alterations of Caney Shale Powders in Field Fracturing Fluids (HF)-XRD analysis
Pyrite breakdown occurs mostly within the first 7 days of reaction
The amount of quartz drops after 7 days but remains relatively constant after that.
Feldspar presence generally shows a downward trend after reaction at both 7 and 30 days
The amount of illite is increasing continuously at 7 and 30 days.
H – Horizontal Well
V – Vertical Well
(7) – 7days reaction
(30) – 30days reaction

## Slide 8
RESULTS - Mineralogical Alterations of Caney Shale Powders in Field Produced Fluids (PF)-XRD analysis
Pyrite breakdown occurs mostly within the first 7 days of reaction
Composition of quartz drops after 7 days but increase between 7 to 30 days
Feldspar composition reduces and completely absent after 30 days
Illite composition shows an increasing trend over 7 days and decrease marginally between 7 & 30 days
H – Horizontal Well
V – Vertical Well
(7) – 7days reaction
(30) – 30days reaction

## Slide 9
RESULTS – Ternary Diagram
General trend of mineralogical transformations due to reaction with fluids
High rate of feldspar, microcrystalline quartz and carbonate dissolution and illite formation in fracturing fluid shifts the mineralogy towards phyllosilicates
High rate of feldspar and microcrystalline quartz dissolution and formation of illite in produced fluid shifts the mineralogy towards phyllosilicates and carbonates in first 7-days of reaction
Subsequent carbonate dissolution coupled with illite breakdown between 7 days and 30 days shifts the mineralogy towards phyllosilicate
Fracturing Fluid
Produced Fluid

## Slide 10
RESULTS - Effluent Analyses (Ca Concentration)
Produced fluid has high initial Ca concentrations
Precipitation or cation exchange in clay sites cause Ca uptake from effluent leading to decreased Ca concentrations
Dissolution of carbonates occur due to transient acidity caused by dissolution of pyrite
Chart: Ca Concentration - PF
| V1 | V2 | V3 | V4 | V5 | H1 | H2 | H3
0 days | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577
7 days | 406614.8321 | 441292.5619 | 403210.5147 | 466723.9245 | 394016.0823 | 421729.7828 | 428776.6468 | 463751.3979
30 days | 431069.7043 | 412014.7063 | 410863.8242 | 439798.5718 | 474640.5789 | 438092.808 | 456574.8855 | 469422.0262
Chart: Ca Concentration - HF
0 days | 64587.6678 | 64587.6678 | 64587.6678 | 64587.6678 | 64587.6678
7 days | 64553.7075 | 79761.0079 | 76438.0926 | 64662.1624 | 67431.3124
30 days | 74269.4737 | 68096.3221 | 76177.1033 | 77720.5657 | 69471.5693
Ca concentrations are relatively stable because, fracturing fluid pH was circumneutral
Dissolution of pyrite causes transient acidity which initiates dissolution of carbonates
Cation exchange in clay sites also causes Ca concentration in effluent

## Slide 11
Dissolution of feldspar contributes to Si concentration in effluent
Dissolved biogenic silica (microcrystalline quartz) and amorphous silica explains the rate of high silica concentrations
Quartz is relatively stable at experimental conditions
Chart: Si Concentration - PF
| V1 | V2 | V3 | V4 | V5 | H1 | H2 | H3
0 days | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354
7 days | 26156.7483 | 39861.674 | 34208.9818 | 26551.1619 | 22421.1461 | 26178.5648 | 40650.5829 | 24740.6883
30 days | 55978.7873 | 56257.7372 | 61934.8532 | 49012.8589 | 42277.2656 | 49179.5693 | 49306.7985 | 51828.4391
Chart: Si Concentration - HF
0 days | 6011.3891 | 6011.3891 | 6011.3891 | 6011.3891 | 6011.3891
7 days | 15838.8159 | 15244.6249 | 17204.3504 | 34429.4148 | 18478.708
30 days | 58376.2917 | 30831.6628 | 27068.3162 | 30624.8211 | 46484.4912
RESULTS - Effluent Analyses (Si Concentration)
High concentrations of Si observed on the graphs cannot be explained by quartz dissolution at the given conditions
Si in effluent is due to dissolution of feldspar and clay minerals
Dissolution of biogenic silica could explain high rate of increase in Si concentrations

## Slide 12
Al is mainly from the dissolution of feldspars and clay minerals
Al concentrations are very low due to uptake from fluid – illite and other Al-based mineral precipitation
Similar trends are observed for Magnesium (Mg) and Iron (Fe)
Chart: Al Concentration - PF
| V1 | V2 | V3 | V4 | V5 | H1 | H2 | H3
0 days | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826
7 days | 170.4136 | 343.7413 | 171.2924 | 162.8403 | 103.8948 | 159.9444 | 156.1593 | 146.5187
30 days | 118.6244 | 102.6724 | 101.3618 | 90.4312 | 91.8806 | 99.3314 | 87.3453 | 84.6583
Chart: Al Concentration – HF
| V2 | V3 | H1 | H2 | H3
0 days | 272.6525 | 272.6525 | 272.6525 | 272.6525 | 272.6525
7 days | 359.2236 | 415.836 | 326.738 | 307.6723 | 309.5257
30 days | 293.9724 | 265.236 | 300.7823 | 300.9494 | 298.3326
RESULTS - Effluent Analyses (Al Concentration)
Al is mainly from the dissolution of feldspars and clay minerals
Al entering solution is precipitated at a fast rate – Illite and Al-based minerals
Similar trends are observed for Magnesium (Mg) and Iron (Fe)

## Slide 13: RESULTS – Model of Experiment
Modeling of experiment shows most elemental concentrations in effluent matching with ICP-MS results
Due to limitations in complete characterization of rock and fluids, assumptions had to be made during the modeling
These assumptions and limitations of model are captured in the next slide

## Slide 14: RESULTS – Model of Experiment
The following uncertainties and limitations are worth noting about modeling of experiment:
Thermodynamic data/models
  Modeled minerals of mixed composition (e.g. clays) may not have the same composition as in the rock formation
  Fluid salinity may exceed the validity range of the implemented ion activity model (extended Debye-Hückel)
Reconstruction of the fluid compositions
  Anion concentrations computed from assumptions Organic compounds besides acetate were neglected (unknown potential effects on experimental results)
Rock formation mineralogy
  Trace or amorphous minerals (undetected by XRD) impact the system geochemistry – amounts and types were assumed
Sampling effects
  Interactions with atmosphere (O2, CO2 impact pH and redox) Mineral reaction rates (kinetic constants, surface area)

## Slide 15: CONCLUSIONS
Conclusions based on integration of results and discussions are as follows:
Caney shale is predominantly composed of quartz, carbonates, illite, plagioclase feldspar, and pyrite
Oxidation is a key driver of rock-fluid reactions
Breakdown of pyrite and other sulfides upon exposure to oxygenated fluids leads to generation of acids which cause localized and transient reduction in pH of fluids, thus catalyzing breakdown of other minerals
Breakdown of minerals causes increased elemental concentrations leading to precipitation of new minerals especially sulfates and carbonates scales and that are detrimental to reservoir permeability
Increasing illite composition transforms an originally brittle rock into a ductile rock consequently easing fracture healing and significantly reducing permeability of reservoir
Increased illite compositions also portents fines generation in the long-term, which can block flow paths and reduce fracture permeability
On the flip side, transformation of originally brittle reservoir rock into a ductile rock over the long-term makes depleted unconventional shale reservoirs good candidates for geological carbon storage

## Slide 16: REFERENCES
Awejori, G. A., Doughty, C., Xiong, F., Paronish, T., Spycher, N., Radonjic, M. (2022). Integrated Experimental and Modeling Study of Geochemical Reactions of Simple Fracturing Fluids with Caney Shale. Energy & Fuels, 36(17), 10064–10081.
Bratcher, J. C., Kaszuba, J. P., Herz-Thyhsen, R. J., Dewey, J. C. (2021). Ionic Strength and PH Effects on Water–Rock Interaction in an Unconventional Siliceous Reservoir: On the Use of Formation Water in Hydraulic Fracturing. Energy & Fuels, 35(22), 18414–18429.
Chakraborty, N., Karpyn, Z. T., Liu, S., Yoon, H. (2017). Permeability evolution of shale during spontaneous imbibition. Journal of Natural Gas Science and Engineering, 38, 590–596.
Farrokhrouz, M., Taheri, A., Iglauer, S., & Keshavarz, A. (2022). The influence of acidizing on propped fractures for productivity enhancement: Eagle Ford laboratory study. Fuel, 329. https://doi.org/10.1016/j.fuel.2022.125363
Jew, A. D., Druhan, J. L., Ihme, M., Kovscek, A. R., Battiato, I., Kaszuba, J. P., Bargar, J. R., Brown Jr, G. E. (2022). Chemical and Reactive Transport Processes Associated with Hydraulic Fracturing of Unconventional Oil/Gas Shales. Chemical Reviews, 122(9), 9198–9263.
Li, Q., Jew, A. D., Kohli, A., Maher, K., Brown Jr, G. E., Bargar, J. R. (2019). Thicknesses of chemically altered zones in shale matrices resulting from interactions with hydraulic fracturing fluid. Energy & Fuels, 33(8), 6878–6889.
Mukhina, E., Cheremisin, A., Khakimova, L., Garipova, A., Dvoretskaya, E., Zvada, M., Kalacheva, D., Prochukhan, K., Kasyanenko, A., Cheremisin, A. (2021). Enhanced oil recovery method selection for shale oil based on numerical simulations. ACS Omega, 6(37), 23731–23741.
Swami, V., Clarkson, C. R., Settari, A. T. (2012). Non-Darcy flow in shale nanopores: do we have a final answer? SPE Canadian Unconventional Resources Conference.

## Slide 17
DOE Award DE-FE0031776 from the Office of Fossil Energy’s, Oil and Natural Gas Program, U.S. Department of Energy
Our industry partners for providing materials and Caney well production histories.

## Slide 18
Please contact us:
gabriel.awejori@okstate.edu
mileva.radonjic@okstate.edu

## Slide 19: THANK YOU

## Slide 20: Back-up Slides

## Slide 21: Subsurface Geochemical Rock-Fluid Reaction in Caney Shale of Southern Oklahoma
Presenter: Gabriel Awejori
Gabriel Awejori1, Wenming Dong2, Christine Doughty2, Nicolas Spycher2, Fengyang Xiong1, and Mileva Radonjic1,3*
1Hydraulic Barrier Materials and Geomimicry Lab, School of Chemical Engineering, Oklahoma State University, Stillwater, Oklahoma, USA
2Energy Geosciences Division, Lawrence Berkeley National Laboratory, 1 Cyclotron Road, Berkeley, CA 94720, USA
3Boone Pickens School of Geology, Oklahoma State University, Stillwater, OK 74078, USA
American Geophysical Union (2023), San Francisco, CA
DOE Award DE-FE0031776 from the Office of Fossil Energy in Partnership with industry partner, OGS, OSU Geology, OSU Chem. Engineering, University of Pittsburgh, Lawrence Berkeley National Lab and DOE NETL.

## Slide 22: ACKNOWLEDGEMENTS
The authors acknowledge:
DOE Award DE-FE0031776 from the Office of Fossil Energy’s, Oil and Natural Gas Program, U.S. Department of Energy
Lisa Whitworth and Brent Johnson of Oklahoma State University Microscopy Laboratory for the support during data acquisition
Our industry partners for providing materials and Caney well production histories.

## Slide 23: DISCUSSION
Trends from mineralogy and effluent analyses reveal significant changes to original compositions of both rocks and fluids
Breakdown of pyrites, carbonates and feldspars leads to increase of elemental concentrations in effluents and in the long-term will aid precipitation of new minerals especially sulfates and carbonates form scales and that are detrimental to reservoir permeability
At high pH, illite becomes unstable and is deflocculated and dispersed, causing clay fines migration. The trends of fluids pH during the reaction shows upward trajectory suggesting the potential of clay fines migration over the long-term
The trends observed from the results show high rate of dissolution of brittle minerals (quartz, pyrite, feldspar) compared to ductile minerals (illite) thus transforming an initially brittle rock into a ductile rock
Feldspar dissolution is proposed as a precursor to the formation of illite?? Another source of illite dominance may be the higher rate of breakdown of brittle minerals
The cumulative impact of reactions described above is the loss of permeability of formation in the long term due to post-hydraulic fracturing rock-fluid interactions.

## Slide 24: INTRODUCTION - Overview of Unconventional Hydrocarbon Reservoirs
Fig. 2: Map showing Locations of unconventional hydrocarbon deposits in the United States of America (https://www.ireservoir.com/case_shale.html, accessed on May 12, 2023)
Unconventional petroleum reservoirs are characterized by ultra low permeability making it difficult to produce from them
In addition to ultra low permeability, unconventional shale reservoirs have high clay content, thus increasing their complexity
However, large reserves of hydrocarbons are stored in these reservoirs.
In the US alone, unconventional reservoirs hold about 6 trillion barrels of oil and 495 trillion cubic feet of gas (Farrokhrouz et al., 2022)
With present technology, only ~10% of hydrocarbons originally in place are recovered from unconventional reservoirs (Mukhina et al., 2021)

## Slide 25: MATERIALS
This work was undertaken using samples recovered from two wells drilled in the Caney Shale
Well 1 is a vertical well drilled through the various zones of the Caney Shale. Samples are thus collected from each of these zones
Well 2 is a horizontal well drilled within Reservoir 3. Samples are therefore collected from comparable depths, 1000ft apart
Main fluid used in experiment was produced fluid from Caney Shale. Deionized water was used as a standard for comparison
Fig. 5: Relative positions of two wells and sample locations: Samples W11 to W15 are cored-rocks from five (5) zones of the formation. W21 to W23 are rock cuttings spaced 1000ft horizontally at approximately the same vertical depth (Schematic not drawn to scale)
W11
W12
W13
W14
W15
W21
W22
W23
Well 1
Well 2
Reservoir
Seal
Reservoir
Reservoir
Seal

## Slide 26: RESULTS – SEM micrographs and EDS Plots
W15_Unreacted_Spots
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
V5_7days_Spots
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
V5_30days_Spots
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
V5_7days_Spots

## Slide 27: RESULTS – SEM Micrographs and EDS Plots
H2_Unreacted_Spot
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
H2_7days_Spot
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
H2_30days_Spot
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si

## Slide 28: RESULTS – SEM micrographs and EDS Plots
Comparison of elemental concentrations on spots selected on unreacted and reacted powdered samples
Microanalysis of all samples are undertaken under the same conditions
Spectrum 6 in all samples is selected to capture the composition of substrate used to hold samples – mainly carbon
Left: Unreacted sample shows highest peaks for elements forming the major minerals identified in XRD measurements - oxygen, silicon, aluminum and calcium
Middle: Samples reacted for 7 days show moderate peaks for major elemental components. This indicates breakdown of minerals or transformation in major minerals
Right: Samples reacted for 30 days show relatively lower peaks for major elements compared to peaks in unreacted and 7 days reacted samples. This is due to continuous reaction and transformation of minerals causing shifts in elemental concentrations
Note:
The shortfall of these measurements is the fact that it is impossible to take spot analyses on the exact particles for both pre-reaction samples and post-reaction samples
However, since particles in powders have comparable mineralogy, multiple spots helps to resolve this issue as much as possible

## Slide 29: RESULTS – Post-Reaction XRD Peaks
The amorphous content after reaction are largely within the clay portions of the XRD peaks
Increased amorphous content after reaction; more evident within the first 7 days
Increased amorphous compositions in the clay section may be due to deflocculation and dispersal of illite
Graph shows XRD diffractograms (right: zoomed-in) of unreacted and reacted samples from W2
XRD peaks of quartz and carbonates showed significant reductions after reacting for 7-days
Reduction due to dissolution of the minerals
i/s
i
q
q
h/ps
d
c
q
q
h/ps
i/s
i
a
q
ii
q
q
c

## Slide 30
RESULTS – Illite Microstructural Identification
TEM Images of unreacted samples showing illite and quartz (Left: 25000x direct magnification. Right: 60000x direct magnification)
Quartz
Illite
Quartz
Illite

## Slide 31
Gabriel Awejori1
Wenming Dong2
Christine Doughty2
Nicolas Spycher2
Fengyang Xiong1
Mileva Radonjic1,3
1 Barrier Materials and Geomimicry Lab, School of Chemical Engineering, Oklahoma State University, Stillwater, OK 74978, USA
2Energy Geosciences Division, Lawrence Berkeley National Laboratory, 1 Cyclotron Road, Berkeley, CA 94720, USA
3Boone Pickens School of Geology, Oklahoma State University, Stillwater, OK 74078, USA
Subsurface Geochemical Rock-Fluid Reaction in Caney Shale of Southern Oklahoma