## Slide 1: Impacts of Geochemical Rock-Fluid Interactions on Production and Carbon Storage in Caney Shale of Southern Oklahoma
Presenter: Gabriel Awejori
Gabriel Awejori1, Wenming Dong2, Christine Doughty2, Nicolas Spycher2, Fengyang Xiong1, Loic Bethel Dje1 and Mileva Radonjic1,3*
1Hydraulic Barrier Materials and Geomimicry Lab, School of Chemical Engineering, Oklahoma State University, Stillwater, Oklahoma, USA
2Energy Geosciences Division, Lawrence Berkeley National Laboratory, 1 Cyclotron Road, Berkeley, CA 94720, USA
3Boone Pickens School of Geology, Oklahoma State University, Stillwater, OK 74078, USA
South-West Regional Meeting - ACS (2023), Oklahoma City, OK
DOE Award DE-FE0031776 from the Office of Fossil Energy in Partnership with industry partner, OGS, OSU Geology, OSU Chem. Engineering, University of Pittsburgh, Lawrence Berkeley National Lab and DOE NETL.

## Slide 2: PRESENTATION OUTLINE
Introduction
Objectives
Materials & Methodology
Results and Discussions
Conclusions
Fig. 1: SEM micrograph of reacted powder sample showing rock grains and clay sized particles. (Ill-Illite, Qtz- Quartz, Cal – Calcite).
Qtz
Ill
Cal

## Slide 3: INTRODUCTION - Overview of Unconventional Hydrocarbon Reservoirs
Fig. 2: Map showing Locations of unconventional hydrocarbon deposits in the United States of America (https://www.ireservoir.com/case_shale.html, accessed on May 12, 2023)
Unconventional petroleum reservoirs have ultra low permeability thus making them challenging to produce from
In case of unconventional shale reservoirs, high clay content adds to the complexity
These reservoirs are estimated to host about 6 trillion barrels of oil and 495 trillion cubic feet of gas in the USA (Farrokhrouz et al., 2022)
With present technology, only ~10% of hydrocarbons originally in place are recovered from unconventional reservoirs (Mukhina et al., 2021)

## Slide 4: INTRODUCTION
Caney Shale is an unconventional shale reservoir in the Ardmore Basin of southern Oklahoma
It generally underlain by the Woodford Shale which is a more prominent producing shale in the area
Though replete with oil and gas, the high clay content and ultra-low permeability creates production challenges
Hydraulic fracturing is therefore undertaken to increase permeability to enable sufficient production
This research is to gain insight on long-term geochemical responses of the Caney Shale after hydraulic fracturing
Fig. 3: Geological map of Oklahoma, showing Sedimentary Basins and well locations (Red Dot within ellipsoid) (after Awejori et al., 2021)

## Slide 5: OBJECTIVES
This study is directed towards investigating the geochemical rock-fluid reactions in subsurface Caney Shale and their impact on long-term permeability in relation to production and carbon storage
To accomplish this objective, crucial sub-objectives are set out to be achieved:
Estimate and understand the general mineralogy of the Caney Shale
Evaluate potential mineralogical transformations in the Caney Shale after hydraulic fracturing
Assess the mechanisms and factors controlling mineralogical transformations after hydraulic fracturing
Fig. 4: Fracture and near-fracture Rock-Fluid Interaction following hydraulic fracturing of reservoir formation

## Slide 6
MATERIALS AND METHODLOGY
Rock Powder
Fluids
Oven
X-ray Diffraction (XRD)
Energy Dispersive Spectroscopy (EDS)
Inductively Coupled Plasma Mass Spectroscopy (ICP-MS)
Before
After
Mineralogical Compositions
Effluent Analyses
Chemical Compositions
Characterization of Alterations caused by Geochemical Reaction
SAMPLE PREPARATION AND STATIC BATCH REACTOR EXPERIMENT
LABORATORY TECHNIQUES AND DATA ACQUISITION
DATA ANALYSES, INTEGRATION AND INTERPRETATION
Vertical Well (Cored-Rock)
Horizontal Well (Rock-Cuttings)
Main Fluid: Field Produced Fluid
Standard: Deionized Water
Conditions: 95oC (203oF), 14.7psi
Liquid to powder ratio (150mL:1g) Average Particle Size =30µm
Sampling Days: 0, 7 and 30 days
Flow chart of materials and methodology used in experiment, data acquisition and interpretation
Simulation
Modeling by LBNL

## Slide 7
RESULTS - Mineralogical Alterations in Well 1 Samples
Pyrite breakdown occurs mostly within the first 7 days of reaction
Quartz drops in the first 7 days but increases between 7 to 30 days whilst carbonate is relatively stable
Feldspar composition reduces and completely breakdown after 30 days
Illite composition shows an increasing trend over 7 days but remains relatively the same between 7 & 30 days
W1 – Vertical Well
W2 – Horizontal Well
(7) – 7 days reaction
(30) – 30 days reaction

## Slide 8
RESULTS - Mineralogical Alterations in Well 2 Samples
Pyrite breakdown occurs mostly within the first 7 days of reaction
Composition of quartz drops after 7 days but increases between 7 to 30 days
Feldspar reduces continuously and mostly dissolve or transform by 30 days
Illite composition shows an increasing trend over 7 days and decrease marginally between 7 & 30 days
W1 – Vertical Well
W2 – Horizontal Well
(7) – 7 days reaction
(30) – 30 days reaction

## Slide 9: RESULTS – SEM micrographs and EDS Plots
Comparison of elemental concentrations on spots selected on unreacted and reacted powdered samples
Microanalysis of all samples are undertaken under the same conditions
Spectrum 6 in all samples is selected to capture the composition of substrate used to hold samples – mainly carbon
Left: Unreacted sample shows highest peaks for elements forming the major minerals identified in XRD measurements - oxygen, silicon, aluminum and calcium
Middle: Samples reacted for 7 days show moderate peaks for major elemental components. This indicates breakdown of minerals or transformation in major minerals
Right: Samples reacted for 30 days show relatively lower peaks for major elements compared to peaks in unreacted and 7 days reacted samples. This is due to continuous reaction and transformation of minerals causing shifts in elemental concentrations
Note:
The shortfall of these measurements is the fact that it is impossible to take spot analyses on the exact particles for both pre-reaction samples and post-reaction samples
However, since particles in powders have comparable mineralogy, multiple spots helps to resolve this issue as much as possible

## Slide 10: RESULTS – SEM Micrographs and EDS Plots
W22_Unreacted_Spot
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
W22_7days_Spot
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
W22_30days_Spot
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si

## Slide 11
RESULTS – Ternary Diagram
Comparison of unreacted samples to 7 days and 30 days reacted samples – Produced Fluids
Ternary diagram gives visual impression of mineral transformation due to rock-fluid reactions
Initial mineralogy of rocks indicate they are brittle; Closer to quartz, feldspar end
Initial higher dissolution of feldspar and microcrystalline quartz shifts the mineralogy towards phyllosilicates and carbonates
Subsequent carbonate dissolution between 7 days and 30 days shifts the mineralogy towards phyllosilicate, quartz, feldspar margin
Shift towards phyllosilicates indicates ductile character is induced into the rock

## Slide 12
RESULTS - Chemical Composition of Caney-Produced Fluids Effluent (ICPMS)
Due to approximate neutral pH, Ca concentrations relatively stable
Dissolution of carbonates occur due to transient acidity caused by dissolution of pyrite
Precipitation or cation exchange in clay sites may lead to Ca uptake from effluent causing decreased Ca concentrations
Chart: Ca Concentration
| W11 | W12 | W13 | W14 | W15 | W21 | W22 | W23
0 days | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577 | 494052.2577
7 days | 406614.8321 | 441292.5619 | 403210.5147 | 466723.9245 | 394016.0823 | 421729.7828 | 428776.6468 | 463751.3979
30 days | 431069.7043 | 412014.7063 | 410863.8242 | 439798.5718 | 474640.5789 | 438092.808 | 456574.8855 | 469422.0262

## Slide 13
RESULTS - Chemical Composition of Caney-Produced Fluids Effluent (ICPMS)
The high Si concentrations cannot be explained only by the dissolution of quartz at the experiment conditions
Dissolved biogenic silica (microcrystalline quartz) and amorphous silica could explain high silica concentrations
Dissolution of feldspar contributes to Si concentration in effluent
Chart: Si Concentration
| W11 | W12 | W13 | W14 | W15 | W21 | W22 | W23
0 days | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354 | 22182.6354
7 days | 26156.7483 | 39861.674 | 34208.9818 | 26551.1619 | 22421.1461 | 26178.5648 | 40650.5829 | 24740.6883
30 days | 55978.7873 | 56257.7372 | 61934.8532 | 49012.8589 | 42277.2656 | 49179.5693 | 49306.7985 | 51828.4391

## Slide 14
RESULTS - Chemical Composition of Caney-Produced Fluids Effluent (ICPMS)
Al is mainly from the dissolution of feldspars
Al concentrations are very low due to uptake from fluid – illite and other Al-based mineral precipitation
Similar trends observed for Magnesium (Mg) and Iron (Fe)
Chart: Al Concentration
| W11 | W12 | W13 | W14 | W15 | W21 | W22 | W23
0 days | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826 | 107.7826
7 days | 170.4136 | 343.7413 | 171.2924 | 162.8403 | 103.8948 | 159.9444 | 156.1593 | 146.5187
30 days | 118.6244 | 102.6724 | 101.3618 | 90.4312 | 91.8806 | 99.3314 | 87.3453 | 84.6583

## Slide 15: RESULTS – Model of Experiment
Modeling of experiment shows most elemental concentrations in effluent matching with ICP-MS results
Due to limitations in complete characterization of rock and fluids, assumptions had to be made during the modeling
These assumptions and limitations of model are captured in the next slide

## Slide 16: RESULTS – Model of Experiment
The following uncertainties and limitations are worth noting about modeling of experiment:
Thermodynamic data/models
  Modeled minerals of mixed composition (e.g. clays) may not have the same composition as in the rock formation
  Fluid salinity may exceed the validity range of the implemented ion activity model (extended Debye-Hückel)
Reconstruction of the Produced Fluid compositions
  Anion concentrations computed from assumptions Organic compounds besides acetate were neglected (unknown potential effects on experimental results)
Rock formation mineralogy
  Trace or amorphous minerals (undetected by XRD) impact the system geochemistry – amounts and types were assumed
Sampling effects
  Interactions with atmosphere (O2, CO2 impact pH and redox) Mineral reaction rates (kinetic constants, surface area)

## Slide 17: DISCUSSION
Trends from mineralogy and effluent analyses reveal significant changes to original compositions of both rocks and fluids
Breakdown of pyrites, carbonates and feldspars release significant elemental concentrations into solution in the long-term to aid in precipitation of new minerals especially sulfates and carbonates that are detrimental to reservoir petrophysical properties
At high pH, illite becomes unstable and is deflocculated and dispersed, thus clay fines migration. The trend of pH of fluids during the reaction shows upward trajectory suggesting the potential of clay fines migration in the long-term
The trends observed from the results show feldspar dissolution and increased illite composition. This trend transforms an initially brittle rock into a ductile rock
Feldspar dissolution is proposed as a precursor to the formation of illite?? Another source of illite dominance may be the higher rate of breakdown of brittle minerals
The cumulative impact of reactions described above is the loss of permeability of formation during long-term post-hydraulic fracturing rock-fluid interactions.

## Slide 18: CONCLUSIONS
The following conclusions are drawn from the integration of results and discussions above:
Caney shale is predominantly made up of quartz, carbonates, illite, plagioclase feldspar, and minor pyrite
Oxidation is a major driver of rock-fluid reactions. Breakdown of pyrite and other sulfides after exposure to oxygenated produced fluid leads to generation of acids which temporarily reduce the pH of fluids, thus catalyzing breakdown of other minerals
High illite compositions implies the potential for fines generation in the long-term, which can occlude flow paths and reduce fracture permeability
Increasing illite composition transforms original brittle rock into a ductile rock consequently helping to heal fractures and significantly reducing permeability of reservoir, thus lost productivity
On the flip side, transformation of relatively brittle reservoir rock into a ductile rock over the long-term makes depleted unconventional shale reservoirs good candidates for geological carbon storage

## Slide 19: ACKNOWLEDGEMENTS
The authors acknowledge:
DOE Award DE-FE0031776 from the Office of Fossil Energy’s, Oil and Natural Gas Program, U.S. Department of Energy
Lisa Whitworth and Brent Johnson of Oklahoma State University Microscopy Laboratory for the support during data acquisition
Our industry partners for providing materials and Caney well production histories.

## Slide 20: REFERENCES
Awejori, G. A., Doughty, C., Xiong, F., Paronish, T., Spycher, N., Radonjic, M. (2022). Integrated Experimental and Modeling Study of Geochemical Reactions of Simple Fracturing Fluids with Caney Shale. Energy & Fuels, 36(17), 10064–10081.
Bratcher, J. C., Kaszuba, J. P., Herz-Thyhsen, R. J., Dewey, J. C. (2021). Ionic Strength and PH Effects on Water–Rock Interaction in an Unconventional Siliceous Reservoir: On the Use of Formation Water in Hydraulic Fracturing. Energy & Fuels, 35(22), 18414–18429.
Chakraborty, N., Karpyn, Z. T., Liu, S., Yoon, H. (2017). Permeability evolution of shale during spontaneous imbibition. Journal of Natural Gas Science and Engineering, 38, 590–596.
Farrokhrouz, M., Taheri, A., Iglauer, S., & Keshavarz, A. (2022). The influence of acidizing on propped fractures for productivity enhancement: Eagle Ford laboratory study. Fuel, 329. https://doi.org/10.1016/j.fuel.2022.125363
Jew, A. D., Druhan, J. L., Ihme, M., Kovscek, A. R., Battiato, I., Kaszuba, J. P., Bargar, J. R., Brown Jr, G. E. (2022). Chemical and Reactive Transport Processes Associated with Hydraulic Fracturing of Unconventional Oil/Gas Shales. Chemical Reviews, 122(9), 9198–9263.
Li, Q., Jew, A. D., Kohli, A., Maher, K., Brown Jr, G. E., Bargar, J. R. (2019). Thicknesses of chemically altered zones in shale matrices resulting from interactions with hydraulic fracturing fluid. Energy & Fuels, 33(8), 6878–6889.
Mukhina, E., Cheremisin, A., Khakimova, L., Garipova, A., Dvoretskaya, E., Zvada, M., Kalacheva, D., Prochukhan, K., Kasyanenko, A., Cheremisin, A. (2021). Enhanced oil recovery method selection for shale oil based on numerical simulations. ACS Omega, 6(37), 23731–23741.
Swami, V., Clarkson, C. R., Settari, A. T. (2012). Non-Darcy flow in shale nanopores: do we have a final answer? SPE Canadian Unconventional Resources Conference.

## Slide 21: THANK YOU

## Slide 22: Back-up Slides

## Slide 23: MATERIALS
This work was undertaken using samples recovered from two wells drilled in the Caney Shale
Well 1 is a vertical well drilled through the various zones of the Caney Shale. Samples are thus collected from each of these zones
Well 2 is a horizontal well drilled within Reservoir 3. Samples are therefore collected from comparable depths, 1000ft apart
Main fluid used in experiment was produced fluid from Caney Shale. Deionized water was used as a standard for comparison
Fig. 5: Relative positions of two wells and sample locations: Samples W11 to W15 are cored-rocks from five (5) zones of the formation. W21 to W23 are rock cuttings spaced 1000ft horizontally at approximately the same vertical depth (Schematic not drawn to scale)
W11
W12
W13
W14
W15
W21
W22
W23
Well 1
Well 2
Reservoir
Seal
Reservoir
Reservoir
Seal

## Slide 24: RESULTS – Post-Reaction XRD Peaks
The amorphous content after reaction are largely within the clay portions of the XRD peaks
Increased amorphous content after reaction; more evident within the first 7 days
Increased amorphous compositions in the clay section may be due to deflocculation and dispersal of illite
Graph shows XRD diffractograms (right: zoomed-in) of unreacted and reacted samples from W2
XRD peaks of quartz and carbonates showed significant reductions after reacting for 7-days
Reduction due to dissolution of the minerals
i/s
i
q
q
h/ps
d
c
q
q
h/ps
i/s
i
a
q
ii
q
q
c

## Slide 25: RESULTS – SEM micrographs and EDS Plots
W15_Unreacted_Spots
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
W15_7days_Spots
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si
W15_30days_Spots
Si
O
Al
Ca
K
Mg
C
Cl
Fe
Na
Si

## Slide 26
RESULTS – Illite Microstructural Identification
TEM Images of unreacted samples showing illite and quartz (Left: 25000x direct magnification. Right: 60000x direct magnification)
Quartz
Illite
Quartz
Illite