## Slide 1: GEOCHEMICAL AND GEOMECHANICAL RESPONSES OF CANEY SHALE TO FRACTURING FLUID COMPOSITIONS AT RESERVOIR CONDITIONS
Presenter: Gabriel Adua Awejori
Awejori, G.A., Fengyang, X., Luo, G., Grider, C., Katende, A., Radonjic, M.
Oklahoma State University, Stillwater, Oklahoma, USA
Doughty, C., Spycher, N.
Energy Geosciences Division, Lawrence Berkeley National Laboratory, Berkeley, California, USA
Paronish, T.
Leidos Research Support Team, National Energy Technology Laboratory, Morgantown, West Virginia, USA
O’Connell, L.
Stim-Lab Inc., Duncan, Oklahoma, USA
Rihn, A.
Continental Resources, Oklahoma City, Oklahoma, USA
DOE Award DE-FE0031776 from the Office of Fossil Energy in Partnership with Continental Resources, OGS, OSU Geology, OSU Chem. Engineering, University of Pittsburgh, Lawrence Berkeley National Lab and DOE NETL.
GSA 2021, PORTLAND, OREGON

## Slide 2: PRESENTATION OUTLINE
Introduction
Objectives
Materials and Methodology
Results
Conclusions and Recommendations
Retrieved Core from Caney Shale on Display

## Slide 3: INTRODUCTION
The Caney shale is a promising unconventional reservoir in South-Central Oklahoma Oil Province (SCOOP)
It overlies the more brittle Woodford Shale which has been the target of drilling over the years
The Caney Shale has been found to contain substantial hydrocarbon deposits
Historically, the Caney Shale has been considered a seal or source rock due to its high clay content
Relatively less work has been done to fully characterize the geochemical and geomechanical responses of the formation to Hydraulic Fracturing Fluids (HFFs)

## Slide 4: OBJECTIVES
Investigate rock responses to HFFs. Key concerns are:
Dissolution and precipitation of Minerals
Clay swelling and Migration of fines
Impact of these on reservoir petrophysical properties

## Slide 5
Characterization of Rock-Fluid Interactions
Modelling (TOUGHREACT)
Batch Experiments
CT Scan and X-Ray Fluorescence
Enable Long-Prediction
From Pore to Core
Experimental and Simulation Design
MATERIALS AND METHODLOGY
X-Ray Diffraction- Mineralogical Composition
Inductively Coupled Plasma-Mass Spectrometry – Effluent Analysis
Scanning Electron Microscopy - Dissolution and Precipitation Patterns

## Slide 6
Fluid Samples and Rock Samples
Three Fluid Compositions: Deionized Water (Base, pH~7), 2% Potassium Chloride Solution (pH~4), and 0.5% Choline Chloride Solution (pH~4)
Three rock samples selected at different depths: High Quartz (HQ), Moderate Quartz, Carbonate and Clay (MQ) and High Clay (HC)
Sample HQ
Sample MQ
Sample HC
MATERIALS AND METHODLOGY

## Slide 7
Which is the main driving force of geochemical reaction?
Fluid composition or Rock Composition?
RESULTS
Impact of Fluid Composition on elemental concentration in effluent
Impact of Rock Composition on Elemental Concentration in effluent

## Slide 8
Ca elemental concentration distinguishable for each fluid type
Ca from Calcite and Dolomite Dissolution
Potassium Chloride>Choline Chloride>Deionized water
HQ and MQ samples have higher concentrations than HC sample
RESULTS

## Slide 9
RESULTS
SO4 elemental concentration distinguishable for each fluid type
SO4 from Dissolution of Pyrite
Potassium Chloride>Choline Chloride>Deionized water
HQ and MQ samples have higher concentrations than HC sample
Chart: HQ
| 1 | 3 | 7 | 14 | 21 | 28
HQDI | 10.649 | 15.642 | 21.623 | 29.333 | 31.7 | 36.045
HQKCl | 23.188 | 30.817 | 35.835 | 40.306 | 39.8 | 43.905
HQCCl | 11.902 | 16.732 | 23.548 | 31.077 | 32.5 | 33.368
Chart: MQ
| 1 | 3 | 7 | 14 | 21 | 28
MQDI | 8.989 | 14.198 | 22.363 | 29.5 | 30.1 | 33.013
MQKCl | 18.173 | 25.431 | 32.078 | 36.243 | 34.7 | 40.563
MQCCl | 12.624 | 17.811 | 26.535 | 33.605 | 33.6 | 35.278
Chart: HC
| 1 | 3 | 7 | 14 | 21 | 28
HCDI | 10.079 | 14.307 | 17.89 | 20.312 | 20.5 | 22.451
HCKCl | 11.511 | 15.372 | 18.007 | 19.557 | 19.2 | 20.711
HCCCl | 9.328 | 13.32 | 17.947 | 21.795 | 21.7 | 22.251

## Slide 10
Si elemental concentration for various fluids clearly distinguishable
Si from Quartz and Clay minerals (Much from Clay Minerals)
Potassium Chloride>Choline Chloride>Deionized Water
Si ions most likely from the clay and feldspathic component of the rock
RESULTS

## Slide 11
Al and Mg are the only elements to show sharp drop in elemental concentrations with time: Precipitation? Possible substitution?
Aluminum elements in solution are from dissolution and cation exchange in clay minerals
Magnesium elemental concentration is mainly from dissolution of dolomite, but clay dissolution and cation exchange in clays also contribute
RESULTS

## Slide 12
Chart: High Clay_DI
pH (25C) | 7 | 8 | 8 | 7.75 | 7.9 | 8.8 | 9.1
Chart: High Clay_KCl
pH meas (25C) | 4 | 7.9 | 8 | 8.1 | 8.6 | 8.9 | 9
Cooled atm CO2 | 4 | 8.054 | 8.071 | 8.097 | 8.122 | 8.138 | 8.088
Except pH values, modelled values and experimental values showed significant disparities
RESULTS
Chart: High Clay _KCl
Al | 0 | 3.6694e-06 | 0 | 0 | 0 | 0 | 0
Chart: High Clay _ KCl
Si | 0 | 0.00033138 | 0.0014883 | 0.0029741 | 0.0033585 | 0.0037422 | 0.0036852

## Slide 13
Three informal Divisions based on XRF results:
Upper Caney shows decreased Si concentration through heavily bioturbated intervals and Al and Fe rich intervals (Clay and Carbonate Rich Zone)
For the middle Caney, Al and Si concentrations remain consistent whilst Ca is low (Quartz-rich shale zone)
In the lower Caney, sharp increase in Ca is observed whilst Al and Si constant (Carbonate zone followed by High Quartz Shale)
RESULTS

## Slide 14: CONCLUSIONS AND RECOMMENDATIONS
Conclusions:
Dissolution and precipitation of minerals during rock-hydraulic fracturing fluid interaction are largely the function of fluid composition
Carbonates and Clays are more susceptible to geochemical reactions whilst Quartz is relatively unaffected by reactions
Increasing clay composition of samples adversely impact the dissolution of quartz and carbonate minerals
KCl and CCl stabilized clay minerals and promotes dissolution of quartz and carbonates
KCl effected greater stabilization of clay minerals thus leaving initially leached elements in solution, therefore higher concentrations
Greater stabilizing effect of potassium chloride may be explained by the greater ability of potassium cations
to exchange for cations in clay interlayers and locking of the interlayers from further interaction with surrounding fluids
Recommendations:
Working on improving geochemical and physical characterization of the rocks and fluid samples for modelling in our next work
Further work will be conducted to explain trends of Al and Mg elemental concentrations: Precipitation? or substitution?
Longer periods for experiments to determine the time limits of KCl and CCl effectiveness in preventing adverse clay-fluid reactions especially considering pH values continued increasing throughout the experiment

## Slide 15: ACKNOWLEDGEMENTS
The authors acknowledge:
DOE Award DE-FE0031776 from the Office of Fossil Energy’s, Oil and Natural Gas Program, U.S. Department of Energy
Joseph Renk, Technical Project Officer, National Energy Technology Laboratory
Lisa Whitworth and Brent Johnson of Oklahoma State University Microscopy Laboratory
Adam Haecker and Barry Dean of Continental Resources for providing Caney well production histories.
The authors would also like to thank George King for guidance
Vissa Vamsikrishna and Cody Massion of Oklahoma State University

## Slide 16: REFERENCES
Dove, P.M. 1995. Kinetic and thermodynamic controls on silica reactivity in weathering environments, in: White, A.F. and Brantley, S.L. (eds). Chemical Weathering Rates of Silicate Minerals. pp. 235–290.
Knauss, K.G., and T.J. Wolery. 1988. The dissolution kinetics of quartz as a function of pH and time at 70 C. Geochim. Cosmochim. Acta 52, 43–53.
Olabode, A.O. 2017. Diagenesis and Formation Stress in Fracture Conductivity of Shaly Rocks; Experimental-Modelling Approach in CO2-Rock Interactions.
Tester, J.W., W.G. Worley, B.A. Robinson, C.O. Grigsby, and J.L. Feerer. 1994. Correlating quartz dissolution kinetics in pure water from 25 to 625C. Geochim. Cosmochim. Acta 58, 2407–2420.